**CABRI 615 PARTITION WALLS**  
  
Doors, partition walls and front walls made of Cabrillant toughened safety glass (ESG) as per EN 12150-2. Float 10 mm, entire surface enamelled using screen printing process, all edges polished smooth. Colours as per standard colour range. Glass height     cm.  
  
Doors, partition walls and front walls made of Cabrillant toughened safety glass (ESG) as per EN 12150-2. Listral SR200, 10 mm, (textured surface), entire surface enamelled, all edges polished smooth. Colours as per standard colour range. Glass height     cm.  
  
Doors, partition walls and front walls made of Cabrillant toughened safety glass (ESG) as per EN 12150-2. Satinato 10 mm (satin finish on one side), entire surface enamelled using screen printing process, all edges polished smooth. Colours as per standard colour range. Glass height     cm.  
  
Doors, partition walls and front walls made of Cabrillant toughened safety glass (ESG) as per EN 12150-2. Float, bright white 10 mm (glass without green cast), entire surface enamelled using screen printing process, all edges polished smooth. Colours as per standard colour range. Glass height     cm.  
  
Doors, partition walls and front walls in Cabrillant laminated safety glass (LSG), comprising 2x 5 mm Float toughened safety glass (ESG) as per EN 12150-2. 1 sheet of glass in centre enamelled over entire surface using screen printing process, 1.52 mm PVB film. Glass height     cm.  
  
Angle brackets used for wall fixing and connection of partition walls with front walls. No visible screw fittings, or  
vertical stabilisers consisting of plain mounting plates in St. 37, 180 x 300 x 8 mm, primed, with clamp arrangement welded on to accept the hot-dip galvanised circular tube with a diameter of 48 mm.  
Steel plate anchored to bare concrete floor. Aluminium tube, clear anodised EV1 placed over steel supports, incl. the necessary connecting elements, height and lateral adjustment possible. Cover rosette in aluminium on ready tiled floor.  
  
Fixed front parts supported by partition wall feet on ready tiled floor. Floor rosettes in solid aluminium. Ground clearance    cm.  
  
In the case of door openings or openings in upper stabilising poles in aluminium EV1, diameter  
25 x 19.  
  
Fittings

In each cubicle: 2 Aluminium alloy door hinges with stainless  
 steel pin and nylon sliding surfaces, incl. integrated spring   
 to hold the doors open  
 1 Olive lock with internal   
 knob and external red/green indicator  
 1 Door stop, theft-proof fitting  
 1 Screen between   
 door hinges on interior  
 1 Screen on lock side, applied on   
 interior.  
  
Alternative: 1 Lock with aluminium handle. External  
 red-green indicator, internal rotary olive handle  
  
 All fittings clear anodised, stainless  
  
Construction parts:  
  
All connecting elements in aluminium (DIN 1725) are 100% corrosion-resistant and environmentally friendly. 100% recyclable.  
  
Enamelled safety glass:  
  
Enamels are lead- and cadmium-free, 100% recyclable.